## Slide 1: Polyolefin Catalysts

## Slide 2
chain of Polyolefin knowledge

## Slide 3: Ziegler Catalysts
Ziegler/Natta Polypropylene Catalysis
TiCl3 Catalysts (First Generation)
The reduction of TiCl4 with an aluminum alkyl, generating a solid TiCl3 precipitate.
TiCl3 exists in four crystalline modifications, α, β, δ, and γ forms. The β-modification has a linear chain-like structure, while α, δ, and γ forms possess layer structures.
Typically, the reaction of TiCl4 and AlEt3 (at low Al/Ti ratios) at low temperatures in hydrocarbon solution resulted in the controlled precipitation of catalysts having spheroidal particle morphology, yielding the β-TiCl3 form with cocrystallized AlCl3.

## Slide 9
This precursor can be converted to the more stereoselective γ-form by heating to 160–200 C [21]. The catalysts were typically activated by AlEt2Cl to afford poorly productive systems (ca. 1 kg PP/g Cat) which
in many cases yielded polypropylene resins that required extractive removal of atactic polymer and removal of catalyst residues (deashing).
TiCl3 Catalysts (Second Generation)
The catalytic activity could be greatly improved by extraction of the co-crystallized aluminum chloride with diisoamyl ether, giving a “pure” β-TiCl3. Subsequent treatment with TiCl4 catalyzed the phase transformation from the β- to the δ-form of TiCl3 at a relatively mild temperature (<100 C) [23]
The innovation increased the activity and stereoselectivity and resulted in
polymerization productivities in the range 5–20 kg/g catalyst in bulk propylene and
produced polymers where the removal of the atactic fraction is spared [24]. Although
phased out in many locations these catalysts still survive to this day

## Slide 13
Third Generation: “Activated” MgCl2
TiCl4 supported on MgCl2
Incorporation into the catalyst system of electron donors giving higher catalyst
stereospecificity
Initially, activated MgCl2 was prepared by ball milling a mixture of magnesium chloride and ethyl benzoate, which leads to the formation of very small (3 nm thick) primary crystallites of MgCl2

## Slide 14
Fourth Generation: Phthalate ID/Alkoxysilane ED
Spherical MgCl2-based catalysts with controlled particle size and porosity, afforded via chemical rather than mechanical activation of magnesium chloride.

## Slide 15
Fifth-Generation Catalysts: Diethers, Succinates, and Polyol Esters
It was found that certain diether compounds, in particular 2,2-disubstituted-1,3-dimethoxypropanes with an oxygen–oxygen distance in the range 2.8–3.2 Å (Fig. 1.3), similar to those of the alkoxysilane external donors are not extracted when the catalyst is brought into contact with the AlEt3 cocatalyst
Fifth-generation diether catalyst systems show particularly high polymerization activity and good stability, typically giving yields exceeding 100 kg PP/g catalyst. They also give relatively narrow molecular weight distribution and show high sensitivity to hydrogen.

## Slide 16
The essential difference between these catalysts is that the succinate-based systems produce polypropylene having much broader molecular weight distribution.
In addition, they also generate ethylene–propylene copolymers having considerably
lower glass transition temperature, coupled with better intermolecular and intramolecular comonomer distribution with respect to their conventional counterparts
production of heterophasic copolymers having an improved balance of stiffness and impact strength, taking into account that the incorporation of a rubbery (ethylene–propylene) copolymer phase into a PP homopolymer matrix increases impact strength but leads at the same time to decreased stiffness

## Slide 17
Sixth-Generation Ziegler: Phthalate Replacement
DOW Consista Donors
1,2-phenylene dibenzoate

## Slide 18
Catalyst Morphology Control
1. Complexation of MgCl2 with an alcohol, forming a viscous melt at elevated
temperature, which is then processed to form a spherical MgCl2EtOHn support
with controllable EtOH content either via spray drying or emulsification/solidification.
The support material is treated with the external donor and titanated to
form the final catalyst product.
2. Complexation of MgCl2 with an alcohol in a hydrocarbon, followed by controlled
precipitation of the reaction products following addition of a chlorinating agent or
TiCl4.
3. Controlled precipitation of the reaction products of a magnesium alkyl or
alkoxide-containing complex with a chlorinating agent or TiCl4.
Finally
4. the impregnation of a silica carrier with the catalyst reagents

## Slide 19
This base material has provided the backbone for
LyondellBasell developments
of Ziegler PP catalyst as well as
Zeigler PE catalyst for gas phase polymerization
Similar carrier material is employed in the
Sinopec/BRICI DQ-catalyst
Novolen
Süd-Chemie

## Slide 21
External Donors

## Slide 23: Ziegler Catalysts: Polyethylene
MgCl2–Titanium Catalysts on Silica
large pore volume and surface area
The silica is either physically impregnated with a solution of MgCl2/TiCl4 in THF
or chemically impregnated with the catalyst components, which can either be added
together or in differing orders. Common practice is to pacify the surface with an
alkyl-aluminum, magnesium complex or an organosilane.
Mobil [189] and UCC [190, 191], respectively. These catalysts, when combined with AlMe3 as a cocatalyst, were the first to produce so called “super-hexene” grade LLDPE, with
improved dart impart strength and hexane extractables
NOVACAT range

## Slide 24
super-hexene” grade LLDPE
With respect to bimodal processes, the silica-based catalysts of Borealis for
Borstar and CX processes have excelled

## Slide 25
Spray-Dried MgCl2–Titanium Catalysts

## Slide 26
MgCl2–Titanium Catalysts Based on Mg(OR)2 HOCHEST Process

## Slide 27
MgCl2–Titanium Catalysts Based on MgCl2 alcohol adducts MITSUIE Process

## Slide 31
Polypropylene Complex Development
Complexes used for copolymerization of propylene with longerchain
olefins (1-butene, 1-hexene, 1-octene etc.)

## Slide 35
Polyethylene Complex Development

## Slide 38
Supported Activator Development
Silica-Supported Methylaluminoxane or Boron-Based Cocatalysts

## Slide 39
Supported Methylaluminoxane System Free of a Support

## Slide 40
Supported Hybrid Catalyst for Multimodal Polyethylene